Do form entail function? Understanding pottery functionalities through absorbed residues within ceramics from the Harappan sites of Karanpura and Ropar in India

Ahana Ghosha, V.N. Prabhakarb, Eleanora. A. Reberd, Helna Listonc, Sivapriya Kirubakaranc, Sreelakshmi K.Sa, Umesh Talekare, Mukesh Bhardwaje, Abhay Vishwakarmae and Sharada Channarayapatnab

Ahana Ghosha

Doctoral scholar

Archaeological Sciences Centre,

Humanities and Social Sciences

Indian Institute of Technology Gandhinagar

Palaj 382355

V.N Prabhakarb

Associate Professor

Archaeological Sciences Centre,

Department of Earth Sciences and Humanities and Social Sciences

Indian Institute of Technology Gandhinagar

Palaj 382355

Eleanora A. Reberd

Professor

Department of Anthropology

University of North Carolina

Wilmington, NC, USA  28403

Helna Listonc

Project Associate,

Department of Chemistry

Indian Institute of Technology Gandhinagar

Palaj 382355

Sivapriya Kirubakaranc

Associate Professor

Department of Chemistry

Indian Institute of Technology Gandhinagar

Palaj 382355

Sreelakshmi K.Sa

Doctoral scholar

Archaeological Sciences Centre,

Humanities and Social Sciences

Indian Institute of Technology Gandhinagar

Palaj 382355

Indian Institute of Technology

Gandhinagar Palaj 382355

Umesh Talekare

Application Manager

Perkin Elmer

Thane 40005

Mukesh Bhardwaje

Senior Application Specialist

Perkin Elmer,

Thane  400059

Abhay Vishwakarmae

Application Specialist

Perkin Elmer,

Thane 400059

Sharada Channarayapatnab

Assistant Professor

Archaeological Sciences Centre,

Departments of Earth Sciences and Humanities and Social Sciences

Indian Institute of Technology Gandhinagar

Palaj 382355

Corresponding Author: Ahana Ghosh

Corresponding Author Email ID: ahanag@iitgn.ac.in

Methodology

The open porosity derived from the Karanpura ceramics was grounded on Archimedes’ principle of liquid immersion. The technique used for measuring open porosity in ceramics involved the use

of a density kit, and the final calculation was executed using the formula mentioned below:

Open Porosity (%)=( ww-dw)/ww-iw)×100

The initials mentioned in the above formula stands for

ww: wet weight

dw: dry weight

iw: immersed weight

Initially, the ceramic sample was cut into smaller pieces using a specialized ceramic cutting machine, followed by the recording of the mass of the dry sample. Next, the sample was soaked in distilled water for an hour until they reached their full saturation level. Following this, the mass of the wet sample was evaluated, and finally, the process was wrapped up with the recording of the mass of the immersed samples from Karanpura.

| Sample ID | Context of the Samples | Vessel Form | Total Lipid Extract (µg lipid/g) | *Open Porosity (%) |
| --- | --- | --- | --- | --- |
| KRN18 | Early Harappan Phase Structural Remains | Incised Ware | 3.4401 | 17.3562 |
| KRN169 | Early Harappan Phase Structural Phase | Cooking Vessel | NA | 24.6724 |
| KRN16 | Early Harappan Mudbrick Structures | Incised Vessel | NA | 24.5996 |
| KRN183 | Structural Phase I Mature Harappan | Cooking Vessel | NA | 20.2227 |
| KRN03 | Structural Phase II Mature Harappan | Incised Ware | NA | 26.5508 |
| KRN187 | Mature Harappan Phase | Cooking vessel | 312.5233 | 19.6164 |
| KRN77 | Mature Harappan Phase | Perforated Jar | 420.7757 | 25.4377 |
| KRN72 | Mature Harappan Phase | Perforated Jar | 141.2201 | 24.2125 |
| KRN13 | Mature Harappan Phase | Incised Ware | 2.6190 | 21.5137 |

Table.1. Comparative analysis of the amount of lipid yield of individual vessels and open porosity from Karanpura

Supplementary information S3.a

| Sample ID | Context of the samples | Vessel Forms | Total Lipid Extract (µg lipid/g) | *Open Porosity (%) |
| --- | --- | --- | --- | --- |
| RPR18 | Locus-039; N5E20 | Cooking Pot | 3.7542 | 19.8 |
| RPR62 | N45-E140 | Cooking Pot | NA | 24.5 |
| RPR153 | N20/W185 | Incised Ware | NA | 31.3 |
| RPR152 | N20/W185 | Cooking Pot | 62.6667 | 21.6 |
| RPR98 | N45E130 | Goblet | 115.4914 | 33 |
| RPR49 | N45- E135 | Perforated Jar | NA | 19.5 |

Table.2. Comparative analysis of the amount of lipid yield of individual vessels and open porosity from Ropar

Supplementary information S3.b